## Slide 1: MAJOR MAINTENANCE & REHABILITATION OF CONCRETE BRIDGES

## Slide 2: Concrete Bridge Decks
Large Percentage of All Bridge Decks (over 90%)
Two Main Mechanisms of Deterioration
  freeze thaw damage
  corrosion of rebar – delamination of concrete
Prevention of Freeze Thaw Damage
  proper concrete mix design and air entrainment

## Slide 3: Concrete Bridge Decks
Prevention of Corrosion Damage
  prevent moisture/chloride entering concrete
  ensure concrete around rebar remains passive
  use non-corrosive rebar
Deck Durability – New Construction
  membrane and ACP
  epoxy coated rebar
  stainless steel/stainless steel clad rebar
  corrosion inhibitors

## Slide 4: Deck Rehabilitation - Timing
Optimum timing gives best life cycle cost
Too early
  existing deck protection still working
  no significant damage to deck
  future life of deck/bridge not shortened if rehabilitation delayed
Too late
  significant corrosion damage to deck
  rehabilitation costs have significantly increased
  high chlorides or other factors have significantly shortened life of deck/bridge
Great deal of experience and judgement to determine optimum timing

## Slide 5: Methods/Options for Rehabilitation
Concrete Overlays
  provides durable long lasting wearing surface
  less permeable – reduces moisture in deck
  reduces rate of corrosion
Waterproofing Membrane and ACP
  waterproofs deck surface
  stops additional moisture getting in deck
  significantly reduces corrosion
  membrane/ACP not as long lasting of a wearing surface as concrete

## Slide 6: Methods/Options for Rehabilitation
Thin Polymer Overlays
  membrane without protection of ACP
  does not add significant dead load
  existing concrete deck in good condition
  need very good bond with concrete
  subject to damage from snow plows, vehicle wear, UV rays

## Slide 7: Methods/Options for Rehabilitation
Cathodic Protection
  electric potential over deck surface prevents additional corrosion
  use when existing corrosion activity very high
  need power source at site
  generally needs to be used with concrete overlay
  monitoring and maintenance required to ensure system is working

## Slide 8: Concrete Overlays

## Slide 9: Types of Concrete Overlay
High Density Concrete
  started using in mid-1970’s
  low water/cement ratio – low slump
  site batched with mobile mixer
  placed with special finishing machine
  very good durability
  less permeable than normal concretes
  still relatively high permeability

## Slide 10: Types of Concrete Overlays
Latex Modified Concrete
  also started using in mid-1970’s
  latex used to replace some of the water in mix
  also site batched
  low permeability/high slump
  can be used for thin overlays < 40 mm
  difficult to finish and cracks easily
  section of overlay can become loose if bonding problems present

## Slide 11: Types of Concrete Overlays
Pyrament Cement Concrete
  cement with high fly ash content – 35%
  on market in early 1990’s
  pre-bag mix – water added at site
  fast setting, high strength, low permeability
  hard to finish – shrinkage cracks
  AAR problems – reduced bond

## Slide 12: Types of Concrete Overlays
Modified Silica Fume Concrete
  small amount of fly ash in mix
  fog curing immediately behind finishing machine
  seven day wet curing
  increase strength – reduces cracks
  can be used with and without steel fibres

## Slide 13: Types of Concrete Overlays
High Performance Concrete (HPC) 45 Mpa – commonly used on AT decks
  Silica fume in mix (6-8%)
  Fly ash in mix (11-15%)
  early use – pre-bag mix – water at site
  presently mostly transit mix
  low permeability – good durability
  little more difficult to finish
  more sensitive to shrinkage cracks when used without fibers
  1st trial deck in Alberta 2022 using 15% lime (GUL replacing GU) BF 1973 – Longview
    Part of “green” initiative – lime more environmentally friendly to produce

## Slide 14: Types of Concrete Overlays
HPC with Steel Fibres
  steel fibres added to mix
  increases tensile strength
  reduces/controls shrinkage cracks
  holds overlay together if debonded
  commonly used in AT overlays

## Slide 26: ACP and Polymer Overlays

## Slide 27: Types of Membrane/ACP
Hot Applied Rubberized Membrane & Protection Board with 2-40 mm Layers ACP (80 mm + 10 mm membrane = 90 mm)
  used on new construction
  dead load limits use for rehabilitation
Sheet Membrane with 50 mm ACP
  repair any damage to deck
  requires fairly smooth surface
  bond with concrete and joints between sheets main concerns
  top of sheet rough surface to protect from and provide bond with ACP

## Slide 28: Types of Membrane/ACP
Polymer Membrane with 50 mm ACP
  requires relatively smooth surface
  good bond with concrete decks
  bond with ACP problem unless some aggregate in top layer
  aggregate can affect permeability of membrane

## Slide 33: Thin Polymer Overlays
Flexible Epoxy Overlays
  two components - must be mixed properly
  can be multi-layer system
  very low permeability
  requires very good preparation of concrete surface
    rough texture but clean
  very sensitive to weather conditions
    concrete internally dry
  even flexible epoxy is a relatively brittle material

## Slide 34: Thin Polymer Overlays
MMA Overlays
  more flexible, thicker material
  single layer
  somewhat more expensive than epoxy
  also requires very good concrete surface preparation
  works better on more flexible decks
Urethane Overlays
  use in parking garages
  not durable enough for highway traffic

## Slide 41: Cathodic Protection Systems
Conductive Wire Mesh in Overlay (Titanium)
  requires concrete overlay
  must eliminate all shorts between mesh and deck
  requires monitoring
Under Deck Conductive Coating
  do not require concrete overlay
  still must eliminate all shorts
  requires monitoring
  long-term performance not proven
  coating system appears to dry out and become non-conductive with time

## Slide 43: Girder Connections and Strengthening

## Slide 44: Lateral Connection Between Girders
AT has a number of concrete girder types that are placed side by side and connected together by grout-keys or connector bolts
These grout keys have not stood up well over time
During rehabilitation of these type bridges the lateral connections are usually upgraded and supplemented (underslung beams, lateral post-tensioning)

## Slide 45: Typical Shear Key – PM Girders

## Slide 46: Grouting Girder Shear Keys

## Slide 47: Lateral Connection Between Girders
Short Span Girders with Bolted Connector Pockets (HC,VS,SM,SL)
  reinforced concrete overlay (nominally 150 mm)
  hair pin bars and grouting
Longer Span Girders (FC, VF, FM)
  lateral stressing
  underslung beams
  combination of both

## Slide 48: Lateral Stressing and Underslung Beam – FC Girders

## Slide 50: Girder Shear Strengthening

## Slide 60: Deck Joints

## Slide 61: Bridge Deck Joints
Pre – 1975 Bridges
  lots of simple spans
  lots of non-waterproof joints
Existing Practice
  continuous spans, eliminate deck joints where possible
  joints waterproof or with drainage systems

## Slide 62: Types of Deck Joints
Strip Seal Joints
  waterproof
  a rubber/neoprene seal attached to metal extrusion
  moderate thermal movements (up to approx. 75 mm)
  make sure installation fills all voids behind extrusions
  work well but seals must be replaced from time to time

## Slide 63: Types of Deck Joints
Finger Plate Joints
  non-waterproof
  sliding finger plates with plumbing/drainage system
  works for large thermal movements (> 75 mm)
  careful to fill all voids behind plates when installing
  mis-alignment of fingers due to dead load creep and abutment rotation
  plumbing/drainage systems need to be cleaned out from time to time

## Slide 64: Types of Deck Joints
Small Movement Joints
  small movements due to live load deflection, etc.
  compression seals
  types of caulking materials

## Slide 72: Full and Partial Depth Deck Repairs

## Slide 76: High Load Repairs – Concrete Girders

## Slide 83: Shotcrete Concrete Repairs

## Slide 90: Curb Concrete Repairs/Replacement

## Slide 95: Concrete Crack Repairs

## Slide 99: Concrete Sealing – Preventative Maintenance

## Slide 104: Specifications for Bridge Construction
Section 4 - Cast in Place Concrete
Section 15 - Polymer Overlays
Section 16 - Bridge Deck Waterproofing
Section 20 – Deck Overlays and Concrete Rehabilitation
Link to Specifications for Bridge Construction:
https://open.alberta.ca/publications/standard-specifications-for-bridge-construction-edition-17

## Slide 105: Questions?