## Slide 1: CULVERT MAINTENANCE

## Slide 2: Culvert Maintenance
Similar to bridges
  approach road
  channel
Structurally different
  upstream end
  downstream end
  barrel

## Slide 3: Maintenance Recommendations
CUL1, CULM and CULE form recommendations are identical

## Slide 4: Maintenance Recommendations
CUL1, CULM, CULE form recommendations are identical

## Slide 5: Approach Road Maintenance
Embankment
  slides, slumps, etc.
    repair by removing failed material & replacement with competent, compacted material
  remaining items same as for bridges

## Slide 6: Upstream / Downstream End Maintenance
Upstream & Downstream ends have the same inspection items
Head Wall
  usually a low maintenance item
  broken, spalled concrete
    patch
  scaled concrete
    repair & seal (when salt applied to roads)

## Slide 7: Upstream / Downstream End Maintenance (Cont’d)
Collar / Concrete Slope Protection
  scoured / eroded
    compacted fill and rock riprap
  settled & broken
    replace with fill and riprap

## Slide 8: Adding end treatment to existing culvert.

## Slide 9: Upstream / Downstream End Maintenance (Cont’d)
Wingwalls
  deteriorated concrete
    chip out and replace
  separated from barrel
    re-connect with steel plates
    fill gap with flexible material
  pushing inwards
    strut between

## Slide 10: Damaged floor at outlet transition.

## Slide 11: Horizontal Steel Strut

## Slide 12: Upstream / Downstream End Maintenance (Cont’d)
Cutoff Wall
  usually buried if present
  if not present and a problem with piping
    Install cut off wall
    Install sand/cement filled bags

## Slide 13: Cement / sand filled bags to repair inlet piping

## Slide 14: Adding cement / sand filled bags to inlet

## Slide 15: Adding cut-off wall to existing culvert.

## Slide 16: Wash out due to piping (Brewster Creek Sunchild Road)

## Slide 17: Upstream / Downstream End Maintenance (Cont’d)
Bevel End
  excessive heaving
    remove and reset with end treatment
    replace with new end treatment
  folding in
    add collar
    strut
  current end treatment requirements are:
    1.5 to 3.0m special conditions
    3.0 to 4.5m upstream end only
    >4.5m both ends

## Slide 18: Bevel pushing inward – repaired with horizontal strut

## Slide 19: Heaved inlet on SPCSP culvert.

## Slide 20: Upstream / Downstream End Maintenance (Cont’d)
Scour Protection
  Erosion / scour
    add suitable size rock riprap with filter cloth to apron and/or around collar or bevel
Scour / Erosion
  scour / erosion
    add rock riprap with filter cloth to suit velocities anticipated

## Slide 21: High velocity at outlet during high water (Bald Mountain Hwy 40)

## Slide 22: Extreme turbulence at outlet.

## Slide 23: Downstream bed erosion and bank erosion at bend.

## Slide 24: Downstream Apron Repair

## Slide 25: Upstream / Downstream End Maintenance (Cont’d)
Rock Riprap Material Size versus Stream Velocity
  Riprap Class Allowable Velocity
  Class 1m - 2.0 m / sec
  Class 1 - 3.0 m / sec
  Class 2 - 4.0 m / sec
  Class 3 - 4.7 m / sec

## Slide 26: Upstream / Downstream End Maintenance (Cont’d)
Degradation
  restore stream bed elevation
  add material
Aggradation
  restore stream bed elevation
  remove material

## Slide 27: Stream degradation and scour hole.

## Slide 28: Hanging outlet due to degradation and scour.

## Slide 29: Typical scour and degradation at outlet

## Slide 30: New rip rap added to bevel and apron

## Slide 31: Streambed aggradation (Cougar Creek Canmore).

## Slide 32: Restored inlet

## Slide 33: Barrel Maintenance
Roof
  Sagging 15% or more
  Reverse curvature
    add struts (might be too late for liner due to reduced hydraulic capacity).

## Slide 34: Reverse curvature in roof

## Slide 35: Barrel Maintenance
Sidewall
  deflecting
    add struts (or install liner if adequate capacity)
  corroded
    Install liner
    cathodic protection (not as common as previously)

## Slide 36: Failed SPCSP culvert (inadequate backfill).

## Slide 37: Soil side corrosion, perforated side wall.

## Slide 38: Barrel Maintenance
Floor
  bulging
    Place U/S cut-off wall if piping
    add struts or install liner
  corroding
    cast concrete floor
    cathodic protection

## Slide 39: Severe Floor perforations

## Slide 40: Floor perforations repaired with concrete floor

## Slide 41: Arch shaped CSP with heaved floor and deflecting roof.

## Slide 42: Strutted barrel

## Slide 43: Concrete arch culvert with curved wingwalls in Feb. (Weed Creek)

## Slide 44: Arch culvert after high water in July.

## Slide 45: Culvert outlet after high water.

## Slide 46: Inlet of new culvert, following winter.

## Slide 47: Hwy. 40 Lineham Creek – Washout of 4.3m SPE – 2013 Flood Event and drift blockage – Showing Outlet

## Slide 48: Hwy. 40 Lineham Creek – Washout of 4.3m SPE – 2013 Flood Event – Inlet blocked by drift

## Slide 49: Hwy. 40 Lineham Creek – Washout of 4.3m SPE – 2013 Flood Event

## Slide 50: Hwy. 40 Lineham Creek – Replacement with 8-14-8M SLW girders in 2015

## Slide 51: Table 11.1 Maintenance Work Types – Culverts & Bridges

## Slide 52: Timber Strutting of Metal Culverts

## Slide 53: Strut detail (Crowfoot Creek Hwy 1).

## Slide 54: Strutting arrangement for a horizontal ellipse.

## Slide 55: Completed installation of adjustable struts

## Slide 56: Culvert Liners

## Slide 57: Installing a CSP liner.

## Slide 58: SPCSP liner is assembled outside and then pulled into an existing culvert.

## Slide 59: For larger culverts, tunnel liner plates are used.

## Slide 60: Liner installed ready for grouting.

## Slide 61: Barrel Maintenance
Circumferential Seams
  separated
    inject concrete or grout
    Install inside coupler plates
Longitudinal Seams
  cracked
    monitor
    shotcrete reinforcement
    cast 1/2 arc concrete
    install liner

## Slide 62: Properly lapped seam.

## Slide 63: Incorrectly lapped seam with poor nesting

## Slide 64: Incorrectly lapped seam with cracks

## Slide 65: Longitudinal Seam Reinforcing

## Slide 66: Reinforcing and shear connectors fastened to culvert.

## Slide 67: Shear connector detail.

## Slide 68: Shear connectors and rebar in place over cracked seam.

## Slide 69: Applying the shotcrete.

## Slide 70: Completed shotcrete reinforcing beams.

## Slide 71: Bottom reinforcement for arch shaped culvert. (Nose Creek Hwy 2)

## Slide 72: Reinforcing installed for arch culvert reinforcement.

## Slide 73: Floor cast inside arch culvert.

## Slide 74: Barrel Maintenance
Coating
  Corrosion
    Soil side corrosion
    Liner
    Water side corrosion
    Concrete floor
    Liner

## Slide 75: Barrel Maintenance (Cont’d)
Fish Passage Adequacy
  add baffles
    cast concrete
    rocks
    weir type
  repair / build downstream apron
Waterway Adequacy
  install additional culvert (jacking)
  remove drift or silt
  install stream lining

## Slide 76: Channel Maintenance
Similar to bridges - Degrading (scour), Aggrading
Drift more of a concern
Beavers are common
High velocities at outlet

## Slide 77: Drift collected at inlet

## Slide 78: Drift in strutted barrel – 100% blockage

## Slide 79: Questions?