## Slide 1: BRIDGE MATERIALS

## Slide 2: CONCRETE
1

## Slide 3: What is Concrete?
2
A mixture of various components which chemically react to form a strong construction material
Unit Weight – normal 2400 kg/m3 or semi 1900 kg/m3
Component Ratios:
  Cement (10 to 15%)
  Aggregate (75 to 80%)
  Water and Air (remainder)
  Admixtures

## Slide 4: Cement Manufacturing
Limestone Train
Clay Quarry
Hammermill Crusher
Preblend Dome
Roller Mill
Preheater Tower
Rotary Kiln
Clinker
Additive Silos
Finishing Mill
Gypsum
Cement Silos
3

## Slide 5: Aggregate
Aggregate qualities for strong and durable concrete:
  Abrasion resistance
  Weather resistance
  Chemical stability
  Cleanliness and even gradation
4

## Slide 6: Water
5

## Slide 7: Entrained Air
Entrained air 5% to 8%
Improves freeze thaw resistance
Improves workability
Reduces segregation and bleeding
Improves sulfate resistance
6

## Slide 8: Air-Entrained Concrete
7

## Slide 9: Admixtures
Ingredients used to modify certain properties of concrete to have a desired function
Two types of admixtures:
  Mineral admixtures
  Chemical admixtures
8

## Slide 10: Mineral Admixtures
Fly Ash
Reduces heat of hydration & increases workability
Increases set time & reduces strength
Silica Fume
Increase strength & abrasion resistance
Increases water demand
Reduces permeability & workability
9

## Slide 11: Chemical Admixtures
Water Reducers – reduces water demand
Super Plasticisers – increases slump, workability, strength
Accelerators – decreases set time
Retarders – increases set time
10

## Slide 12: Physical Properties
Compressive strength (f’c) (28 day)
Tensile strength (10% f’c)
Shear strength (12-13% f’c)
Flexural strength (14% f’c)
11

## Slide 13: Physical Properties (Cont’d)
How to increase Compressive Strength
Increased cement content
Increased aggregate strength
Decreased w/c ratio
Decreased entrapped air
Increased curing time
Use of admixtures
12

## Slide 14: Concrete Stress-Strain Diagram
strain
stress
13

## Slide 15: Physical Properties (Cont’d)
Creep
Fire resistance
Durability
Isotropy
Permeability
  Affected by
    evaporation of bleed water
    excess water
    micro-cracking
    porous aggregates
    improper mixing, finishing
14

## Slide 16: Concrete Damage & Deterioration
CRACKS
Crack is a linear fracture in concrete
  Working Cracks
  Structural Cracks
    Flexure cracks
    Shear cracks
15

## Slide 17: Structural Cracks
Flexural Cracks
Flexural Cracks
Unloaded Beam
Shear Cracks
16

## Slide 18: Concrete Damage & Deterioration
  Non-Structural Cracks
    Crazing cracks
    Temperature cracks
    Shrinkage cracks
  Crack Size
    Hairline less than 0.1 mm
    Narrow ≥ 0.1 mm < 0.3 mm
    Medium ≥ 0.3 mm < 1.0 mm
    Wide ≥ 1.0 mm
17

## Slide 19: Shrinkage Cracks on Deck Underside.
18

## Slide 20: Concrete Damage & Deterioration
2. SCALING
Scaling is a gradual loss of mortar and aggregate
Categories of Scaling
  Light scaling loss of surface mortar 6 mm deep
  Medium Scaling loss of surface mortar 6 to 13 mm deep
  Heavy scaling coarse aggregate exposed
  Severe scaling loss of coarse aggregate
19

## Slide 21: Light Scaling
20

## Slide 22: Medium Scaling
21

## Slide 23: Heavy Scaling
22

## Slide 24: Freeze/Thaw Deterioration of Deck
23

## Slide 25: Concrete Damage & Deterioration
3. POP-OUTS
Due to porous aggregate
4. ABRASION
Due to wheel wear
5. SPALLING
Expansion of corroding rebar and overstressing
24

## Slide 26: Expansive Aggregate Pop-out
25

## Slide 27: Abrasion Damaged Girders
26

## Slide 28: Concrete Damage & Deterioration
6. DELAMINATION
Bond failure between old and new concrete and expansion of corroding rebar
7. STAINING
Rust stains leaching through cracks
8. ALKALAI AGGREGATE REACTION
9. CARBONATION (EFFLORESCENCE)
27

## Slide 29: Delamination Mechanism
Reinforcement
Top of concrete
Wearing surface
Corrosion by-products
28

## Slide 30: Delamination & Corroded Rebar
29

## Slide 31: Longitudinal Crack & Corroding Rebar
30

## Slide 32: Corrosion Spall
350
31

## Slide 33: Calcium Carbonate Deposits
32

## Slide 34: Concrete - Steel Combination
Reinforced Concrete
  Concrete has high compressive strength and low tensile strength
  Always cracks under tensile load
  Mild steel carries tensile load
Prestressed Concrete
  High strength steel strands
  Concrete is pre-compressed
  Carries load without cracking
33

## Slide 35: STEEL
34

## Slide 36: What is Steel?
Steel is an alloy of iron, carbon and other trace metals
Carbon and trace metal ratios:
  Carbon 0.15 to 0.3%
  Manganese 0.50 to 2.0%
  Phosphorus 0.02 to 0.2%
  Sulphur 0.02 to 0.06%
  Silicon 0.15 to 0.8%
35

## Slide 37: Iron
Iron in the pure form is a soft, shiny metal like aluminum.
However, it is never found in this state.
Iron oxidizes extremely easily.
In nature it is always found as an oxide.
36

## Slide 38: Steel Making Process
Iron ore, coke and limestone are major raw materials.
Raw material is charged into Blast furnace which has a temperature of 1600°C.
Iron melts and settles at the bottom.
Solidified iron is called “Pig Iron”
37

## Slide 39: Steel Making Process
Molten metal from blast furnace and silicon is taken into Basic Oxygen furnace
Chemical analysis of the molten material is done
Steel billets are heated to 1200C for rolling and finished products.
38

## Slide 40
39

## Slide 41
Molten Iron
40

## Slide 42: Effects of Various Elements
Effects of Carbon in steel:
  Increases strength and hardness
  Reduces ductility, weldability, machinability and toughness
Effects of Phosphorus in steel:
  Increases strength and hardenability
  Reduces ductility and weldability
41

## Slide 43: Effects of Various Elements
Effects of Manganese in steel:
  Increases strength, hardenability and notch toughness
  Reduces weldability
  Reduces ill effects of sulfur
Effects of Sulfur in steel:
  May cause porosity and hot cracking in welding
  Can cause brittleness
42

## Slide 44: Effects of Various Elements
Silicon in steel:
  Increases strength, hardenability and notch toughness
  Reduces weldability
  Deoxidizer in steel making
Copper, Chrome, Nickel:
- Weathering steel (Cor-ten)
43

## Slide 45: Common Steel Shapes
  Wires
  Cables
  Steel Plates
  Steel Bars
  Rolled Beams
  Built-up Shapes
44

## Slide 46: Rolled Sections
Angle
Channel
Rolled I Beam
45

## Slide 47: Built-up Sections
46

## Slide 48: Important Physical Properties
Strength
  Compression
  Tension
  Fatigue
Ductility
Notch toughness
Weldability
Fire Resistant
Corrosion Resistant
47

## Slide 49: Tension & Compression
lengthen (+)
Stress Strain Diagram
tension
shorten (-)
compression
(-)
(+)
48

## Slide 50: Steel Damage and Deterioration
Corrosion
  Environmental corrosion
  Stray current corrosion
  Stress corrosion
Cracking
  Fatigue
  Impact
  Excessive loading
Note: Any crack in a steel member is serious
49

## Slide 51: Steel Damage and Deterioration
Deformation
  Excessive loading
  Heat damage
  Impact
50

## Slide 52: Corrosion Holes in Girder Web
51

## Slide 53: Stains from Soil Side Corrosion
52

## Slide 54: Crack initiated by Bolt Hole
53

## Slide 55: Collision damaged steel girder.
54

## Slide 56: Fire Damaged Truss.
55

## Slide 57: Fire Damaged Truss.
56

## Slide 58: UNCONTROLLED WELDING IS NOT ALLOWED ON BRIDGE STRUCTURES.
57

## Slide 59: TIMBER
58

## Slide 60: Wood
What is wood?
  A naturally occurring non- homogeneous material.
Composition of timber:
  Carbohydrate fibres
  Water
Classification of timber:
  Hardwood
  Softwood
59

## Slide 61: Cross Section of Tree
Outer Bark
Cambium
Rays
Pith
Heartwood
Inner Bark
Sapwood
60

## Slide 62: Growth Features
Growth features
  Knots
  Splits, Checks
Moisture content
  Moisture affects dimensional stability
  19% moisture content is considered seasoned wood
61

## Slide 63: Checks
62

## Slide 64: Physical Properties
Compression
    perpendicular to grain
    parallel to grain
Tension
Bending
Fatigue
Shrinkage
    60% radially
    2% longitudinally
63

## Slide 65: Timber Damage & Deterioration
Abrasion
Warping
Checks & Splits
Cracking
  Flexural
  Horizontal Shear
Fire Damage
Collision Damage
Decay
64

## Slide 66: Timber Damage & Deterioration
Decay is caused by fungi
To grow fungi need:
  Oxygen
  Temperature
  Food
  Moisture
Insects – Pine beetles can be a serious problem in Alberta
65

## Slide 67: Protective Systems
Water repellents
Preservatives
  Creosote
  Cromated Copper Arsenate (CCA)
  Ammoniacal Copper Zinc Arsenate (ACZA)
Paint
66

## Slide 68: Warping due to Drying Shrinkage
67

## Slide 69: Horizontal Shear Crack.
68

## Slide 70: Checking & Start of Rot
69

## Slide 71: Serious Rot in Stringer
70

## Slide 72: Fire Damaged Timber
71

## Slide 73: Questions??
72