## Slide 1: BRIDGE MATERIALS

## Slide 2: CONCRETE

## Slide 3: What is Concrete?
A mixture of various components which chemically react to form a strong construction material
Unit Weight – normal 2400 kg/m3 or semi 1900 kg/m3
Component Ratios:
  Cement (10 to 15%)
  Aggregate (75 to 80%)
  Water and Air (remainder)
  Admixtures

## Slide 4: Cement Manufacturing
Limestone Train
Clay Quarry
Hammermill Crusher
Preblend Dome
Roller Mill
Preheater Tower
Rotary Kiln
Clinker
Additive Silos
Finishing Mill
Gypsum
Cement Silos
4

## Slide 5
Aggregate qualities for strong and durable concrete:
  Abrasion resistance
  Freeze/thaw resistance
  Chemical stability
  Cleanliness and even gradation
Aggregate
5

## Slide 6: Water

## Slide 7: Entrained Air
Entrained air 5% to 8%
Improves freeze thaw resistance
Improves workability
Reduces segregation and bleeding
Improves sulfate resistance

## Slide 8: Air-Entrained Concrete

## Slide 9: Admixtures
Ingredients used to modify certain properties of concrete to have a desired function
Two types of admixtures:
  Mineral admixtures
  Chemical admixtures

## Slide 10: Mineral Admixtures
Fly Ash
Reduces heat of hydration & increases workability
Increases set time & reduces strength
Silica Fume
Increase strength & abrasion resistance
Increases water demand
Reduces permeability & workability
Limestone
First used in trial project in 2022. GU replaced with GUL (up to 15%)
Part of a “green initiative”, more environmentally friendly to produce.

## Slide 11: Chemical Admixtures
Water Reducers – reduces water demand
Super Plasticizers – increases slump, workability, strength
Accelerators – decreases set time
Retarders – increases set time

## Slide 12: Physical Properties
Compressive strength (f’c) (28 day) (e.g. HPC = 45 Mpa)
Tensile strength (6 to 7% f’c)
Shear strength (12-13% f’c)
Flexural strength (14% f’c)

## Slide 13
How to increase Compressive Strength
Increased cement content
Increased aggregate strength
Decreased water/cement ratio
Decreased entrapped air
Increased curing time
Use of admixtures
Physical Properties (Cont’d)

## Slide 14: Concrete Stress-Strain Diagram
strain
stress
Notes: LK - Linear Elastic Region: Stress and strain are proportional, and concrete behaves as a linearly elastic material. The member should be able to retain its original shape if load is removed. The slope of this section is the modulus of elasticity (E). Typically, linearly up to 0.45 f’c
Transition Region: Concrete begins to strain beyond elastic region and begins to exhibit plastic deformation.
Plastic Region: the concrete deforms plastically, and the stress-strain curve levels off (or peaks), which indicates the maximum compressive stress. The concrete is no longer able to withstand additional stress at this point.

## Slide 15: Physical Properties (Cont’d)
Creep
Fire resistance
Durability
Isotropy
Permeability
  Affected by
    evaporation of bleed water
    excess water
    micro-cracking
    porous aggregates
    improper mixing, finishing

## Slide 16: Concrete Damage & Deterioration
1. CRACKS
A crack is a linear fracture in concrete
Working Cracks
Structural Cracks
  Flexure cracks
  Shear cracks

## Slide 17: Structural Cracks
Flexural Cracks
Flexural Cracks
Unloaded Beam
Shear Cracks

## Slide 18: Concrete Damage & Deterioration
Non-Structural Cracks
Crazing cracks
Temperature cracks
Shrinkage cracks
Crack Size
Hairline less than 0.1 mm
Narrow ≥ 0.1 mm < 0.3 mm
Medium ≥ 0.3 mm < 1.0 mm
Wide ≥ 1.0 mm

## Slide 19: Map Cracking in Concrete Deck

## Slide 20: Shrinkage Cracks in Concrete Curb

## Slide 21: Hairline Transverse Crack in Sidewalk

## Slide 22: Concrete Damage & Deterioration
2. SCALING
Scaling is a gradual loss of mortar and aggregate
Categories of Scaling
Light scaling loss of surface mortar 6 mm deep
Medium Scaling loss of surface mortar 6 to 13 mm deep
Heavy scaling coarse aggregate exposed
Severe scaling loss of coarse aggregate

## Slide 23: Light Scaling

## Slide 24: Medium Scaling
Notes: Aggregate starting to become partially visible

## Slide 25: Heavy Scaling

## Slide 26: Freeze/Thaw Deterioration of Deck

## Slide 27: Concrete Damage & Deterioration
3. POP-OUTS
Due to porous aggregate
4. ABRASION
Due to wheel wear
5. SPALLING
Expansion of corroding rebar and overstressing

## Slide 28: Expansive Aggregate Pop-out

## Slide 29: Abrasion Damaged Girders

## Slide 30: Concrete Damage & Deterioration
6. DELAMINATION
Delamination is the separation of the paste layer within concrete (i.e. an internal crack). Delamination leads to spalling. Typically caused by the volumetric expansion of corroding rebar.
7. STAINING
Includes rust, efflorescence, or water stains leaching through cracks
8. ALKALAI AGGREGATE REACTION
9. CARBONATION
10. EFFLORESCENCE

## Slide 31: Delamination Mechanism
Reinforcement
Top of concrete
Wearing surface
Corrosion by-products

## Slide 32: Delamination & Corroded Rebar

## Slide 33: Longitudinal Cracks & Corroded Rebar

## Slide 34: Spalled Concrete – Corroded Rebar and Broken Stirrup

## Slide 35: Calcium Carbonate Deposits

## Slide 36: Concrete - Steel Combination
Reinforced Concrete
Concrete has high compressive strength and low tensile strength
Typically cracks under tensile load
Traditional reinforcing steel (rebar) carries tensile load
Prestressed Concrete
Use of both rebar and high-strength steel strands
Concrete is pre-compressed as a result of pre-tensioning the steel strands
Carries load without cracking

## Slide 37: STEEL

## Slide 38: What is Steel?
Steel is an alloy of iron, carbon and other trace metals
Carbon and trace metal ratios:
Carbon 0.15 to 0.3%
Manganese 0.50 to 2.0%
Phosphorus 0.02 to 0.2%
Sulphur 0.02 to 0.06%
Silicon 0.15 to 0.8%

## Slide 39: Iron
Iron in the pure form is a soft, shiny metal like aluminum.
However, it is never found in this state.
Iron oxidizes extremely easily.
In nature it is always found as an oxide.

## Slide 40: Steel Making Process
Iron ore, coke and limestone are major raw materials.
Raw material is charged into Blast furnace which has a temperature of 1600°C.
Iron melts and settles at the bottom.
Solidified iron is called “Pig Iron”
Molten metal from blast furnace and silicon is taken into Basic Oxygen furnace
Chemical analysis of the molten material is done
Steel billets are heated to 1200°C for rolling and finished products.

## Slide 41: Bridge Materials

## Slide 42: Bridge Materials
Molten Iron

## Slide 43: Effects of Various Elements
Effects of Carbon in steel:
Increases strength and hardnessand improves hardenability
Reduces ductility (brittleness increases), toughness, machinability and weldability once heat treated
Effects of Phosphorus in steel:
Increases strength and hardenability
Reduces ductility and weldability

## Slide 44: Effects of Various Elements
Effects of Manganese in steel:
Increases strength, hardenability and notch toughness
Reduces weldability
Reduces ill effects of sulfur
Effects of Sulfur in steel:
May cause porosity and hot cracking in welding
Can cause brittleness

## Slide 45: Effects of Various Elements
Silicon in steel:
Increases strength, hardenability, and notch toughness
Reduces weldability
Deoxidizer in steel making
Certain amounts of silicon can considerably affect hot-dip galvanizing
Copper, Chrome, Nickel:
Weathering steel (Cor-ten)

## Slide 46: Common Steel Shapes
Wires
Cables
Steel Plates
Steel Bars
Rolled Beams
Built-up Shapes

## Slide 47: Rolled Sections
Angle
Channel
Rolled I Beam

## Slide 48: Built-up Sections

## Slide 49: Important Physical Properties
Strength
  Compression
  Tension
  Fatigue
Ductility
Notch toughness
Weldability
Fire Resistant
Corrosion Resistant

## Slide 50: Tension & Compression
lengthen (+)
Stress Strain Diagram
tension
shorten (-)
compression
(-)
(+)

## Slide 51: Steel Damage and Deterioration
Corrosion
Environmental corrosion
Stray current corrosion
Stress corrosion
Cracking
Fatigue
Impact
Excessive loading
Steel may also crack when flows are present, especially if near the surface.
Note: Any crack in a steel member is serious

## Slide 52
Deformation
Excessive loading
Heat damage
Impact
Steel Damage and Deterioration

## Slide 53: Corrosion Perforations in Tie Plate – BF 9315

## Slide 54: Soil Side Corrosion in Culvert Barrel

## Slide 55: Crack initiated by Bolt Hole

## Slide 56: Crack in post base initiated by expanding frozen water

## Slide 57: Crack in post initiated by expanding frozen water

## Slide 58: Collision damaged steel girder.

## Slide 59: Fire Damaged Truss

## Slide 60: Fire Damaged Truss.

## Slide 61
UNCONTROLLED WELDING IS NOT ALLOWED ON BRIDGE STRUCTURES

## Slide 62: TIMBER

## Slide 63: Wood
What is wood?
A naturally occurring non- homogeneous material.
Composition of timber:
Carbohydrate fibres
Water
Classification of timber:
Hardwood
Softwood

## Slide 64: Cross Section of Tree
Outer Bark
Cambium
Rays
Pith
Heartwood
Inner Bark
Sapwood

## Slide 65: Growth Features
Growth features
Knots
Splits, Checks
Moisture content
Moisture affects dimensional stability
19% moisture content is considered seasoned wood

## Slide 66
Occur naturally
Not generally considered a defect in timber
Can be differentiated from cracks by the presence of creosote or other preservatives visible on the inside surface of the check
Cracks that have formed after application of the wood preservative will have not have preservative present at the inside surface.
Checks

## Slide 67: Physical Properties
Compression
  perpendicular to grain
  parallel to grain
Tension
Bending
Fatigue
Shrinkage
  60% radially
  2% longitudinally

## Slide 68: Timber Damage & Deterioration
Decay and fungal growth
Abrasion
Warping
Splits
Wide checks or checks within wet / dry zone of pile (> 25 mm)
Cracking
  Flexural
  Horizontal Shear
Fire Damage
Collision Damage

## Slide 69: Timber Damage & Deterioration
Decay is caused by fungi
  Fungi need the following to grow:
    Oxygen
    Temperature
    Food
    Moisture
  Fungal growth will not occur while wood remains submerged under water or buried deep in ground (oxygen depleted environments).
Insects – Pine beetles can be a serious problem in Alberta

## Slide 70
Water repellents
Preservatives
  Creosote
  Cromated Copper Arsenate (CCA) – green color
  Alkaline Copper Quaternary (ACQ) – brown color
  Ammoniacal Copper Zinc Arsenate (ACZA)
Paint
Protective Systems

## Slide 71: Warping due to Drying Shrinkage

## Slide 72: Horizontal Shear Crack.

## Slide 73: Fungal Growth and Beginning Rot

## Slide 74: Rot in Stringer End

## Slide 75: Fire Damaged Timber

## Slide 76: Questions?